VWR Sterile Coverall CAT III Type 5/6

60g SMS, with Hood, Elastic Wrist, Ankle and Back, Zip down Front,

Zipper Bi Directional, Thumb Loop at Sleeves, Bound Seams, aseptic donning design

Intended use

Sterile cleanroom production or research

General Sepcification

| Item | Test method | Standard |
| --- | --- | --- |
| Material | - | 60g SMS |
| Color | - | White |
| Zipper | - | Nylon |
| Elastic | - | Thumb loop : latex free Rest : latex |
| BFE (Bacterial Filtraction Efficiency) | ASTM F2101 | >90.5% |
| Particle Shedding | IEST-RP-CC003.3 (≥0.5μm/cu. ft.) | 409 Level I |
| Sterilization | ISO11137 | SAL10-6 |
| Surface resistivity (Ω) | EN1149-1:2008 | <2.5*109 |

Material Specifications

1. 60gsm SMS

| Item |  | Test method | average value standard |  |
| --- | --- | --- | --- | --- |
|  |  |  | average value | tolerance for average value |
| Weight(g/m2) |  | GB/T4669-1995 | 60.00 | +/-3 |
| Thickness(mm) |  | ASTM D1777 | 0.184 | +/- 0.02 |
| Break Tensile propertities(N) | MD | ASTM D5034 | >60 |  |
|  | CD | ASTM D5034 | >35 |  |
| Elongation rate(%) | MD | ASTM D5034 | >30 |  |
|  | CD | ASTM D5034 | >30 |  |
| Tear prosperities | MD | ISO9073-4 | >30 |  |
|  | CD | ISO9073-4 | >30 |  |
| Hydrostatic press test (mmH2O) |  | AATCC127 | >450 |  |
| Air permeability test (mm/s) |  | ISO9073-15 | >200 |  |
| Surface resistivity (Ω) |  | EN1149-1:2008 | <2.5*109 |  |

Dimension Specification

| EU Cat. No. | SIZE | A | B | C | D | E | F | G | H | I | J |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 113-7881 | S | 166 | 57 | 85 | 28 | 8/18 | 12/24 | 29 | 72 | 35 | 15 |
| 113-7882 | M | 169 | 60 | 86 | 28 | 8/18 | 12/24 | 32 | 73 | 35 | 15 |
| 113-7883 | L | 176 | 63 | 90 | 28 | 8/18 | 12/24 | 35 | 82 | 40 | 15 |
| 113-7884 | XL | 178 | 66 | 92 | 28 | 9/20 | 13/26 | 36 | 82 | 40 | 15 |
| 113-7885 | XXL | 186 | 74 | 98 | 28 | 9/20 | 13/26 | 39 | 82 | 45 | 15 |
| 113-7886 | XXXL | 192 | 79 | 99 | 28 | 9/20 | 13/26 | 43 | 85 | 45 | 15 |
| Tolerance |  | ±2 | ±2 | ±2 | ±2 | ±1/±2 | ±1/±2 | ±1 | ±2 | ±3 | ±1 |

Packaging Specification

| Package/Quantity | 1pcs/pe bag/pe bag, 20pcs/case liner/case |
| --- | --- |
| Best storage Conditions | 0- 50°C |
|  | 45% - 65% humidity |
|  | dry |
| Shell Life | 5 years |
| Country of Origin | China |

Product Compliance:

ISO 13485:2003 Medical device-Quality management system-requirements for regulatory

EN 13034:2005+A1:2009 Protective clothing against liquid chemicals – Performance requirements for chemical protective clothing offering limited protective performance against liquid chemicals

EN ISO 13982-1:2004+A1:2010 Protective clothing for use against solid particulates-Part1: Performance requirements for chemical protective clothing providing protection to the full body against airborne solid particulates

EN1149-5:2008: Protective clothing - Electrostatic properties - Part 5: Material performance and design requirements

Disclaimer: VWR wants to state that this declaration will not discharge the user from his obligation to ensure the product is suitable for the intended use. -  If there is any doubt ask us.

Date of issue: Dec 2021